Pos.:……..

Surface box made of plastic according to DIN 4056, certified by the DVGW-German Technical and Scientific Association for Gas and Water

Maintenance-free non-adjustable finish for the assembly of lock-up and water armatures

Dimensions and cover weight according to DIN 4056.

Base body is made of glass-fiber reinforced plastic.

Plastic material must be oil and road salt proof.

All components have to be recyclable.

The mounted surface boxes must bear up a pressure load of 200 kN.

Heat resistant up to 245°C

Cover made of cast iron EN- JL 1030 (GG- 20), sustainably corrosion-resistant.

Cover screw joint is made of X5CrNi 1810 steel.

The bolt is made of chrome steel with a minimum chrome part of 13%.

Manufacturer quality like Serius or similar

Item………

€/Item……..								€/Total………..

Pos.: ….

Supporting plate made of plastic for surface box 4056.

Supporting plate according to the manufacturer of the surface box

Item……

€/Item………								€/Total………..