Pos.:……..

Surface box made of plastic according to DIN 4059, certified by the DVGW-German Technical and Scientific Association for Gas and Water

Maintenance-free adjustable finish for the assembly of house connections

Dimensions and cover weight according to DIN 4059.

Base body is made of glass-fiber reinforced plastic.

Plastic material must be oil and road salt proof.

All components have to be recyclable.

The mounted surface boxes must bear up a pressure load of 200 kN.

Heat resistant up to 245°C

In order to guarantee a steady adjustability during the construction phase, intrusion of impurities between the base body and the adjuster has to be avoided with the help of a respective sealing.

The edges of the adjuster have to be flush settable.

An incline of 4° between the base body and the adjuster on approx. 50% of the extracted part has to be possible for the alignment of the level.

The adjuster must be fixable without forceful impact in any reasonable position.

Cover made of cast iron EN- JL 1030 (GG- 20), sustainably corrosion-resistant.

Cover screw joint is made of X5CrNi 1810 steel.

The bolt is made of chrome steel with a minimum chrome part of 13%.

Manufacturer quality like Serius or similar

Item……..

€/Item………..								€/Total…………..

Pos.:………

Supporting plate made of plastic for surface box DIN 4059, adjustable

Supporting plate according to the manufacturer of the surface box

Item……..

€/Item………………							€/Total……………..